FACT SHEET

GP550 Series - TPE for sealing strips



MANUFACTURER OF TPE&TPR

SOLUTIONS IN SOFT TOUCH MATERIALS

|  |  |
| --- | --- |
| Typical Applications* Sealing strip
 |  |
|   |  |

|  |  |  |  |
| --- | --- | --- | --- |
| **Physical Property** | **Unit** | GP550-5504 | GP550-7504 |
| Hardness | Shore | 55A | 75A |
| Density | g/cm3 | 1.1 | 1.1 |
| Tensile Strength | MPa | 4.5 | 7.0 |
| Elongation at Break | % | 600 | 550 |

   

Our Know-how – Your Advantage

With smooth and soft touch, excellent elasticity, UV resistant, good weldability, fully recyclable features, GP550 can be used to produce a variety of sealing strip.

具行业内符合最高质量标准。 无论是彩色的，高透明度的，抗撕裂的还是特

**Safety first:**

**Standards that meet market requirements:**

**Contains no latex, PVC, phthalates or heavy metals**

**Soft, dry surface**

**Very good sensory properties and low migration levels**

**Durability:**

Excellent mechanical properties, such as good elasticity, resistance to yellowing

Hardness ranges from Shore A 45 to Shore A 95

Technical Data

TALK TO OUR EXPERTS！

**SUNGLORY PLASTIC (VIET NAM) COMPANY LIMITED - SOUTHEAST ASIA**

 Candy@sungallon.com