FACT SHEET

GP610 Series – TPE for automotive seals, door and window seals



MANUFACTURER OF TPE&TPR

SOLUTIONS IN SOFT TOUCH MATERIALS

|  |  |
| --- | --- |
| Typical Applications   * Automotive seals * Door and window seals |  |
| Free Mercedes-Benz Car photo and picture | Free Car Vehicle photo and picture |

|  |  |  |  |
| --- | --- | --- | --- |
| **Physical Property** | **Unit** | GP610-4502 | GP610-8502 |
| Hardness | Shore | 45A | 70D |
| Density | g/cm3 | 0.96 | 0.96 |
| Tensile Strength | MPa | 4.0 | 9.0 |
| Elongation at Break | % | 420 | 520 |



Our Know-how – Your Advantage

With excellent aging resistance, high resilience, excellent compression resistance, halogen-free, fully recyclable features, GP610 can be used for safe automotive seals, door and window seals.

具行业内符合最高质量标准。 无论是彩色的，高透明度的，抗撕裂的还是特

**Safety first:**

**Standards that meet market requirements:**

**Contains no latex, PVC, phthalates or heavy metals**

**Halogen-free**

**Durability:**

Temperature resistance

Excellent mechanical properties, such as good elasticity, aging resistance, compression deformation resistance

Hardness ranges from Shore A 40 to Shore A 90

Technical Data

TALK TO OUR EXPERTS！

**SUNGLORY PLASTIC (VIET NAM) COMPANY LIMITED - SOUTHEAST ASIA**

 Candy@sungallon.com