FACT SHEET

GP410 Series - TPE for toy figures and foamed shoe materials

MANUFACTURER OF TPE&TPR

SOLUTIONS IN SOFT TOUCH MATERIALS

| Typical Applications - Toy figures - Vent toy | - Stress relief ball - Foamed shoe materials |
| --- | --- |

| Physical Property | Unit | GP410-35 | GP410-9202 |
| --- | --- | --- | --- |
| Hardness | Shore | 35A | 92A |
| Density | g/cm3 | 0.94 | 0.98 |
| Tensile Strength | MPa | 3.5 | 12.1 |
| Elongation at Break | % | 700 | 450 |

Our Know-how – Your Advantage

With high tension, high torque, high elasticity, easy coloring and paintable, fully recyclable features, GP410 can be used for safe toy figures and foamed shoe materials.

具行业内符合最高质量标准。 无论是彩色的，高透明度的，抗撕裂的还是特

Safety first:

Standards that meet market requirements:

Food grade contact requirements;

Contains no latex, PVC, phthalates or heavy metals

Durability:

Excellent mechanical properties, such as good tear resistance and tensile strength, high elasticity

Hardness ranges from Shore A 10 to Shore A 95

Technical Data

TALK TO OUR EXPERTS！

SUNGLORY PLASTIC (VIET NAM) COMPANY LIMITED - SOUTHEAST ASIA

Candy@sungallon.com