FACT SHEET

GP510 Series – TPE for toy tire leather, handle, sheet gasket

MANUFACTURER OF TPE&TPR

SOLUTIONS IN SOFT TOUCH MATERIALS

| Typical Applications - Toy tire leather - Sheet gasket | - Handle |
| --- | --- |

| Physical Property | Unit | GP100-50A | GP100-70A |
| --- | --- | --- | --- |
| Hardness | Shore | 50A | 70A |
| Density | g/cm3 | 1.06 | 1.15 |
| Tensile Strength | MPa | 4 | 3.2 |
| Elongation at Break | % | 600 | 500 |

Our Know-how – Your Advantage

With resistant to high tension, high elasticity, easy to process, fully recyclable features, GP510 can be used for safe toy tire leather, handle, sheet gasket.

具行业内符合最高质量标准。 无论是彩色的，高透明度的，抗撕裂的还是特

Safety first:

Standards that meet market requirements:

Passed FDA177.2600 water-based test and GB4806.7 food-grade test;

Contains no latex, PVC, phthalates or heavy metals

Soft surface

Very good sensory properties and low migration levels

Durability:

Excellent mechanical properties, such as good tensile strength and high elasticity

Hardness ranges from Shore A 10 to Shore A 95

Technical Data

TALK TO OUR EXPERTS！

SUNGLORY PLASTIC (VIET NAM) COMPANY LIMITED - SOUTHEAST ASIA

Candy@sungallon.com